## Slide 1
Beam Profile Measurements of Decelerated Multicharged
Xe Ions from ECRIS for Estimating Low Energy
Damage on Satellites Components
24th International Workshop on ECR Ion Sources
Koichi Sato, Kazuki Okumura, Shuhei Harisaki,
Wataru Kubo, Issei Owada, Kazuki Tsuda, and Yushi Kato
Division of Electrical, Electronic and Inforcommunications Engineering,
Graduate School of Engineering, Osaka University

## Slide 2
Background
Low-Energy Sputtering
[1]JAXA–RR–09–004, pp.26--31 ,2010
Theory
Experimental data
☞Low energy sputtering yield has some different results in experimental data and theory.
☞ In designing satellites for 10-15 years of operation, low
energy sputtering cannot be ignored.
・Xe+：80%
・Dependence of incidence angle
The irradiation experiment is carried out using
a device that simulates an ion engine.
1

## Slide 3
Background
～ In our laboratory ～
・ Experimental setup using an existing ECRIS for decelerated ion beams
・ Improvement of beam line to increase current
Previous studies
Our goal is measurement of sputtering yield by irradiating satellite components with low energy Xe ion beam.
2
The amount of beam currents is not enough for irradiation
when the extraction voltage is 1kV and Xe is extracted.
We extract the ion beams from high voltage 10 kV and transported
into the ion beam irradiation system (IBIS) where we constructed.
And we decelerate and irradiate ion beams to the materials.
Beam Deceleration

## Slide 4
Objective
Construction of equipment for irradiation experiment
・ Xe, Ar Deceleration Experiments
→Measurements of beam current in the low energy region
・Measurements of beam profiles in the low energy region
・ Calculations of the current density ＆ Evaluating of the dose amount
→ Estimation of irradiation time
・ Problem: Uniformity of beam profile on the sample about 1cm2
⇒We measure the two dimensional profiles of the decelerated beam
3

## Slide 5
ECRIS ＆ Beam line
Steering Coil 2
Steering Coil 1
4

## Slide 6
Ion Beam Irradiation System (IBIS)
FCi
Irradiation
target
Insulator
X-Y Wire Probe
Casing
Insulator
300
5

## Slide 7
Construction of equipment for irradiation experiment
6
FCi
Irradiation
target
Insulator
X-Y Wire
Probe
Casing
Deceleration electrodes
beam
X-Y Probe and FCi
with casing in detail
Beam irradiation part

## Slide 8
FCi
Irradiation
target
Insulator
X-Y
Wire Probe
Casing
Deceleration electrodes
Beam irradiation part
beam
Construction of equipment for irradiation experiment
Movement of the X-Y wire probe during
measurements of two dimensional profiles
7

## Slide 9
Xe Deceleration Experiment
Experimental Results
We found that there was
sufficient current to conduct
irradiation experiments in the
low energy region (100～200eV).
8
FC Beam Current [µA]
FCi Beam Current [µA]
FCi Beam Current [µA]

## Slide 10
Measurements of Decelerated Xe+ Ion Beam Profiles
9
Experimental Results

## Slide 11
Future Plan
☞ We succeeded in acquiring the profile of decelerated beam.
Summary and Future Plan
Summary
☞ Sufficient beam current in the low energy region (about 100eV
to 500eV) for irradiation experiments
☞ Irradiation experiments for various materials
☞ Further improvement of deceleration electrode and irradiation
system to shorten irradiation time
☞ Evaluation of high precision dose amount and irradiation time
10

## Slide 12
Construction of equipment for irradiation experiment
FCi
Irradiation
target
Insulator
X-Y
Wire Probe
Casing
Deceleration electrodes
Beam irradiation part
beam
FCi
Target
X-Y Wire Probe
Casing
Ion Beam
y[cm]
Beam Current[µA]
x [cm]
Beam Current[µA]
6

## Slide 13
FCi
Irradiation
target
Insulator
X-Y
Wire Probe
Casing
Deceleration electrodes
Beam irradiation part
beam
Construction of equipment for irradiation experiment
XY-Probe
(Mo φ0.5)
FCi (φ50)
Casing
Target
outlet
7

## Slide 14
FCi
Irradiation
target
Insulator
X-Y
Wire Probe
Casing
Deceleration electrodes
Beam irradiation part
beam
We calculate the beam area using the full width at
half maximum (FWHM) in the X and y directions.
Current density calculation procedure
re Probe
X-Y Wire Probe
X-Y Wire Probe
Construction of equipment for irradiation experiment
7

## Slide 15
1.1 Ar Deceleration Experiment
Experimental Results
#2020/07/09
We found that there was
sufficient current to conduct
irradiation experiments in the
low energy region (100～200eV).
8

## Slide 16
1.2 Measurements of Decelerated Ar+ Ion Beam Profiles
Experimental Results
9
※(FWHM)
※(FWHM)

## Slide 17
照射部
D3
100mm
0
Decelerating electrodes
Experiment method of beam deceleration
FCi
Casing
Decelerating
electrodes
D2
D1
D3
配線

## Slide 18
2．Construction of equipment for irradiation experiment
FCend
Irradiation
target
Insulator
X-probe (wire probe)
Casing
Deceleration electrodes
Setup of preliminary experiment for design of equipment
Experiment method of beam deceleration
beam
Beam irradiation part
X-probe
Casing
・X-probe can be rotated to
measure the x direction.
・The probe and the casing can be floated to GND by the insulator, and these can be applied with a deceleration voltage VD3.
X-probe

## Slide 19
Chart: 
| 2.3492315519647713 | 1.915111107797445 | 1.6069690242163484 | 1.2500000000000002 | 0.85505035831417209 | 0.43412044416732598 | 0.21788935686914535 | 1.531435568635775E-16 | -0.2178893568691456 | -0.43412044416732576 | -0.85505035831417175 | -1.2499999999999996 | -1.6069690242163484 | -1.9151111077974448 | -2.3492315519647708
 | -0.05 | -0.04 | 0 | 0.19 | 1.21 | 1.36 | 1.36 | 1.43 | 0.65 | -0.05 | -0.05 | -0.05 | -0.05 | -0.05 | -0.05
 | 0.1 | 0.08 | 0.07 | 0.07 | 0.06 | 0.06 | 0 | 0 | 0 | 0 | 0 | 0
 | 0.1 | 0.08 | 0.07 | 0.07 | 0.06 | 0.06 | 0 | 0 | 0 | 0 | 0 | 0
 | 0.42 | 0.43 | 0.85 | 1.27 | 1.2 | 0.58 | 0.32 | 0.02 | 0 | 0 | 0
x [cm]
Beam current [µA]
#2019/11/08
Vel2=7.66 kV
Vel3=6.6 kV
10 keV
1 keV
100 eV
Xe+
B∝m/q
Xe+
Beam Current [μA]
Xe2+
Xe3+
#2019/11/08
Pressure: 4.0×10-4 Pa
VPE=10kV
Microwave power:140W/130W
measurement: FC(50 mmφ)
Slit：40 mm
0
10
20
30
40
50
60
70
☞ We obtained the beam profile in the x direction from 100eV to 10keV.
☞ It was found that the beam trajectory shifted when beam was decelerated.
The beam profile in the x direction from 100eV to 10keV
2．Construction of equipment for irradiation experiment

## Slide 20
3．Construction of equipment for irradiation experiment
FCi
Irradiation
target
Insulator
Dual-Probe
Casing
Deceleration electrodes
Beam irradiation part
beam
Step.1 Dual-Probe can be rotated to measure the x direction
And be pulled out to measure the y direction.
Step.2 Even when the target is inserted, it does not come into contact with the probe.
Calculation method of current density

## Slide 21
Chart: 
| -1.5 | -1.25 | -1 | -0.75 | -0.5 | -0.25 | 0 | 0.25 | 0.5 | 0.75 | 1 | 1.25 | 1.5
 | -0.02 | 0.05 | 0.19 | 0.37 | 0.62 | 1.33 | 4.4 | 4.21 | 2.09 | 0.5 | 0 | 0 | 0
 | -0.03 | -0.04 | -0.04 | -0.04 | -0.05 | 0 | 0.09 | 0.46 | 1.08 | 1.18 | 0.75 | 0.33 | 0.03
Chart: 
| -1.5 | -1.25 | -1 | -0.75 | -0.5 | -0.25 | 0 | 0.25 | 0.5 | 0.75 | 1 | 1.25 | 1.5
 | -0.01 | -0.01 | 0 | 0 | 1.7 | 3.86 | 2.96 | 2.73 | 1.6 | 0.87 | 0.44 | 0.06 | 0
 | -0.04 | -0.03 | -0.03 | -0.03 | -0.02 | -0.01 | 0 | 0.94 | 2.62 | 0.27 | 0.44 | 0.3 | 0.04
Chart: 
| -1.5 | -1.25 | -1 | -0.75 | -0.5 | -0.25 | 0 | 0.25 | 0.5 | 0.75 | 1 | 1.25 | 1.5
 | -1.0063 | -0.75472 | -0.75472 | -0.75472 | -0.50314 | -0.25157 | 0 | 23.6478 | 65.9119 | 6.7925 | 11.0692 | 7.5472 | 1.0063
 | -0.29851 | -0.29851 | 0 | 0 | 50.7463 | 115.2239 | 88.3582 | 81.4925 | 47.7612 | 25.9701 | 13.1343 | 1.791 | 0
Chart: 
| -1.5 | -1.25 | -1 | -0.75 | -0.5 | -0.25 | 0 | 0.25 | 0.5 | 0.75 | 1 | 1.25 | 1.5
 | -1.791 | -2.3881 | -2.3881 | -2.3881 | -2.9851 | 0 | 5.3731 | 27.4627 | 64.4776 | 70.4478 | 44.7761 | 19.7015 | 1.791
 | -0.44444 | 1.1111 | 4.2222 | 8.2222 | 13.7778 | 29.5556 | 97.7778 | 93.5556 | 46.4444 | 11.1111 | 0 | 0 | 0
Operation check of the manufactured device
2．Production of equipment for irradiation experiment
x [cm]
Beam current [µA]
y [cm]
Beam current [µA]
x [cm]
y [cm]
Calculating the current density using the full width at half maximum(FWHM)…
current density[µA/cm2]
current density[µA/cm2]
500 eV
10 keV
10 keV
500 eV
500 eV
10 keV
10 keV
☞ In the FCi, the current density using these FWHM were 79.6 µA/cm2(1keV) and 85.2µA/cm2(500eV). When performing the irradiation experiment on Si with Ar+ using this current density, it can be performed in about several tens of minutes.
500 eV
Ar+
Ar+
Ar+
Ar+

## Slide 22
減速時にビーム偏向する理由
Setup and method of irradiation experiment
Steering Coil 2
Is2
上面図
側面図
電流の向き
Is1
上面図
側面図
Steering Coil 1

## Slide 23
減速時にビーム偏向する理由

## Slide 24
ビームプロファイル測定結果
Beam Current [μA]
x[cm]
y[cm]
Xe+(500eV)
Xe+(500eV)→Si
2020/01/08
Xe+(500eV)
Xe+(500eV)→Si
照射実験

## Slide 25
3. 照射実験
段差測定結果
center
Left
Right
ターゲット材料
マスク部分